Quote text TFD Experiece 3-6

| Pos. |  | Product description |
| --- | --- | --- |
| 1. |  | General information TFD Experience 3-6 heterogeneous, elastic floor plank with wood look; floor covering made from heterogeneous PVC in accordance with ISO 10582. ..............m² TFD Experience 3-6 Format according EN 427: 22.8 x 149,8 mm x 2.5mm Thickness of wear layer ISO 24340: 0.55 mm Total thickness ISO 24346: 2.5mm Basic weight ISO 23997: ca 4.2 kg/m² Dim. stability ISO 23999: 0.05% Noise absorption ISO 10140-1: ca. 4 dB Residual indentation ISO 24343-1: 0.04 mm. Burning behaviour ISO 13501-1: Bfl-s1 Usage classification 10582: 23/33/42 Slip resistance DIN 51130: R10 Colour according to client’s specifications The sub-floor must be inspected in accordance with VOB part C DIN 18356 before installation. The under-surface must be level, tear-free, dry, clean and sturdy, in accordance with requirements in DIN 18202 “Tolerances in high-rise buildings“. Use in accordance with supplier’s installation instructions. Cleaning and maintenance in accordance with supplier’s recommendations. Origin: TFD Floortile ### TFD Floortile B.V. De Vesting 2 7722 GA Dalfsen Netherlands T: +31 529 431466 info@tfd-floortile.com www.tfd-floortile.com |